---

title: "NEAT: A Python Toolkit for Neutron Bragg-Edge Imaging Data Analysis"

tags:

- Python

- neutron imaging

- Bragg edge

- materials characterization

- strain mapping

- open-source software

authors:

- name: Ruiyao Zhang

orcid: 0000-0002-5557-5210

affiliation: 1

- name: Ranggi Ramadhan

orcid: 0000-0003-1256-7015

affiliation: 1

- name: Manuel Morgano

orcid: 0000-0001-6195-5538

affiliation: 1

- name: Scott Young

affiliation: 1

- name: Winfried Kockelmann

orcid: 0000-0003-2325-5076

affiliation: 1

- name: Sylvia Britto

orcid: 0000-0003-1515-307X

affiliation: 1

affiliations:

- name: ISIS Neutron and Muon Source, Rutherford Appleton Laboratory, Harwell, United Kingdom

index: 1

date: 2025-11-03

bibliography: paper.bib

---

# Summary

**NEAT (Neutron Bragg-Edge Analysis Toolkit)** is an open-source Python graphical user interface (GUI) [@Zhang2025] that enables scientists to analyse neutron imaging data without advanced programming experience.

Neutron imaging uses beams of neutrons to look inside solid objects in a non-destructive way, revealing how atoms are arranged and how materials deform under stress [@Santisteban2001]. When a neutron beam passes through a crystalline solid, sharp changes—called *Bragg edges*—appear in the transmitted intensity as a function of neutron wavelength. The position and shape of these edges provide information about lattice spacing, elastic strain, phase composition, and microstructure [@Ramadhan2022].

**NEAT** offers a complete and user-friendly environment to transform raw neutron time-of-flight images into quantitative maps of material properties. It combines data cleaning, correction, fitting, and visualisation steps into a single tool, reducing the need for multiple scripts or external software.

The program is particularly suited for experiments performed at energy-resolved neutron imaging instruments such as **IMAT (ISIS, UK)**, but can also be used with data from similar facilities worldwide like **RADEN (J-PARC, Japan)** [@Shinohara2016], and **POLDI (PSI, Swiss)** [@Polatidis2020].

# Statement of Need

Bragg-edge neutron imaging (NBEI) is increasingly used to study residual stress, deformation, and phase transformation in engineering components, cultural artefacts, and advanced manufactured parts. Despite its growing importance, analysis tools remain fragmented—often requiring manual scripting for each stage of data processing.

Existing packages such as **RITS** [@Sato2011], **TPX_EdgeFit** [@Tremsin2016], **BEATRIX** [@Minniti2019], and **iBeatles** [@Bilheux2025] address parts of the workflow, but none integrate pre-processing, fitting, and map visualisation in one open-source, cross-platform environment.

**NEAT** was developed to fill this gap by providing:

- A consolidated pipeline from raw detector frames to strain or phase maps, all within a single GUI;

- A robust analytical model using a **pseudo-Voigt Bragg-edge function** and a modified three-stage optimisation strategy for stable fitting;

- A *pattern-fitting* mode that refines multiple edges simultaneously to obtain a global lattice parameter, analogous to Pawley refinement in diffraction;

- High-throughput mapping with **pixel-skip** and **macro-pixel** options for rapid feedback during beamtime.

Validation on benchmark iron samples at the IMAT beamline demonstrated that NEAT accurately reproduced the expected tensile–compressive strain fields and microstructural variations, while reducing analysis time from hours to minutes.

The tool has since been applied to projects on additively manufactured superalloys, residual-stress mapping, and cultural-heritage specimens.

# Functionality Overview

- **Automated preprocessing:** run summation, pixel cleaning, overlap (pile-up) correction, and normalisation with optional binary masking.

- **Edge fitting:** individual or multi-edge pattern fitting using pseudo-Voigt profiles to extract lattice spacing, strain, edge width, and edge height.

- **Post-processing and visualisation:** immediate 2-D maps and line-profiles of fitted parameters for interpretation and publication.

# Example of Use

To demonstrate NEAT’s workflow, we analysed Bragg-edge imaging data collected from U-shaped iron specimens measured at the IMAT beamline (ISIS, UK). The sample was bent to U-shape from a straight bar, leaving residual stress / strain in the bend [@Haribabu2024].

The raw time-of-flight image stacks were loaded into NEAT, where the runs were automatically summed, cleaned, and normalised using the built-in preprocessing pipeline.

After selecting the Fe-bcc phase, a macro-pixel region was defined to extract the transmission spectrum, and the 110, 200, and 211 Bragg edges were fitted using both single-edge and multi-edge (“pattern”) modes with a pseudo-Voigt profile.

The automated batch-fitting routine then produced two-dimensional maps of lattice spacing, Bragg-edge width, and edge height across the sample within minutes.

The resulting lattice-parameter map revealed tensile regions (red) along the inner bend and compressive regions (blue) along the outer bend, consistent with the expected plastic bending behaviour (*Figure 1*). In addition to strain mapping, NEAT quantifies Bragg-edge width and height, which provide complementary information on microstructural evolution due to plastic deformation induced by bending.

![Example](https://github.com/RayZhang2024/NEAT/blob/main/docs/paper/Example.png)

**Figure 1:** From left to right, fitted lattice parameter, 110 edge width and 110 edge height of the U-shape bent sample.

# Acknowledgements

This work was supported by the **Engineering and Imaging Group** at the **ISIS Neutron and Muon Source**, Science and Technology Facilities Council (STFC), United Kingdom.

The authors thank **Computing Division** at ISIS Neutron and Muon Source and **Scientific Computing Department** of STFC for their technical support, and the **IMAT user community** for their valuable feedback during development and testing.

# References